## Slide 1
Design Optimization, Additive Manufacturing Technologies & applications| 5th Computational Methods and Ocean Technology (COTech 2026)
Explainable Artificial Intelligence and Supervised Machine Learning for Surface Roughness Prediction of Additively Manufactured PLA Specimens
Kifle Mesfin*
Bahir Dar University, Ethiopia
CENTRAL FINDING
XGBoost captured 96.34% of the variation in measured PLA surface roughness.
0.9634
R²
0.0558
MSE
0.1992
MAE
Research question
Can surface roughness in FDM-printed PLA be predicted accurately while keeping the model transparent enough for engineering decisions?
Surface roughness influences wear, reliability, appearance, and the structural performance of additively manufactured components.
Experimental design
• 30 PLA specimens generated by response surface methodology
• ASTM E8 geometry uniformly reduced by 50%
• Surface roughness averaged across four measurement locations
• Mitutoyo SJ-10 tester used for the response measurement
Thirty printed PLA specimens
Creality FDM printing setup
Scaled ASTM E8 specimen geometry
Eight process inputs
Layer height
Wall thickness
Infill density
Infill pattern
Nozzle temperature
Bed temperature
Print speed
Fan speed
Machine-learning workflow
01 RSM trials → 02 Eight inputs → 03 80/20 split → 04 Nine regressors → 05 XAI interpretation
SVR • Decision Tree • Random Forest • XGBoost • CatBoost • AdaBoost • Extra Tree • Gradient Boosting • Explainable Boosting Machine
Nine-model benchmark
Chart: 
| CatBoost | Decision Tree | EBM | SVR | AdaBoost | Gradient Boosting | Extra Tree | Random Forest | XGBoost
R² | 0.63163 | 0.67314 | 0.7504 | 0.82296 | 0.89432 | 0.90492 | 0.90671 | 0.91893 | 0.96342
XGBoost predicted vs. actual values
Best overall model
XGBoost
Lowest MSE and MAE, and the highest R² among all nine regressors.
What the benchmark means
Tree-based ensembles dominated the comparison. Random Forest, Extra Tree, Gradient Boosting, and AdaBoost all achieved R² values near or above 0.89, but XGBoost produced the clearest improvement in prediction accuracy.
Evaluation metrics: mean squared error (MSE) | mean absolute error (MAE) | coefficient of determination (R²)
Explainable AI reveals process influence
SHAP values connect each process setting to the direction and magnitude of its contribution to the predicted surface roughness.
XGBoost SHAP beeswarm: global feature impact
SHAP heatmap: instance-level feature contributions
Interpretation
• Layer height showed the widest SHAP spread and the strongest overall influence.
• Print speed was the second most influential input.
• Infill density and wall thickness showed moderate, instance-dependent effects.
• Bed temperature, fan speed, and infill pattern contributed less within the investigated design space.
1 Accurate
XGBoost achieved R² = 0.9634.
2 Interpretable
SHAP exposed how each process input affected prediction.
3 Actionable
Layer height and print speed are priority controls.
Kifle Mesfine|*
jowalt965@gmail.com